## Slide 1: Towards High Energy 10 fs Laser Pulse via Regenerative pulse shaping
P.M. Paul, L.Vigroux, G. Riboulet, F.Falcoz

## Slide 2: Broadband Amplifiers: Regenerative Pulse shaping
Main Limitation in High gain Amplifier: Gain Narrowing
Ti:Sa
Pockels cell
FWHM<35 nm
SOLUTION REGENERATIVE PULSE SHAPING
Barty et al. Opt.Lett. Vol.21, No.3, pp.219-221 (1996)
Barty et al. Opt.Lett. Vol.21, No.9, pp.668-670 (1996)

## Slide 3: Broadband Amplifiers: Regenerative Pulse shaping
Global Amplifier Gain
l
Goal: Flattest Amplifier
Spectral Gain
Ti:Sa
Pockels cell
Spectral
filter
 Regenerative pulse shaping via Intracavity Spectral Filter

## Slide 4: Broadband Amplifiers: Regenerative Pulse shaping
Ti:Sa
Pockels cell
Spectral
filter
Thin etalon
birefringent filter
spatial mask
multiple dielectric layers
-Pulse Replica
-Cavity instability
-Programmability ?


## Slide 5: Acousto-Optique Programmable Gain Control Filter (Mazzler)
Ti:Sa
Pockels cell
Spectral filter
Acousto-Optic Programmable Gain Control Filter (AOPGCF)
acoustic wave
non-diffracted beam
diffracted beam
Brewster incidence angle
collinear interaction geometry (efficiency and resolution)
very easy calibration

## Slide 6
10 mJ
10 Hz
High Dynamic Third order cross-correlator Sequoia
APE SPIDER
pump
Oscillator
AOPDF (DAZZLER )
P1
P2
Faraday
TFP
TFP1
TFP2
Stretcher
Compressor
AOPGCF
Pre-Amplifier
Ultrabroadband regenerative amplifiers via AOPGCF : Experiments

## Slide 7
a
80 nm
Spectrum Optimization
After the loop the spectrum obtained is around 80nm
The spectral width is limited by the bandwidth of theoptics (100nm)

## Slide 8

- Low residual losses
- No contrast deterioration, no pulse replica
- Complete software programmability
Easy installation and calibration
-Simple and direct bandwidth optimization :35nm  >120nm
-Optimization automation possible
-Stability and reliability

- Dispersion of the TeO2 crystal => >200000 fs3 to compensate
=> Needs to be coupled with a DAZZLER
Ultrabroadband regenerative amplifiers via AOPGCF : Conclusions

## Slide 9: Ultra Broadband Amplifier
Up to 120-130 nm bandwidth can be obtained
Using 200 nm-Broadband optics, the Mazzler approach can be extended to Ultra broadband spectra
10 fs
Optics Reflectivity > 200 nm
The FFT of the spectrum gives a pulse duration around 10fs

## Slide 10: Ultra Broadband Amplifier
Chart: 
The seeded bandwidth is now limited by the stretcher transmission  130 nm
The broadband optics have improved the output spectrum
However we clearly see some clipping effects on the stretcher output
Do we amplify the all spectrum of the oscillator ?

## Slide 11: Ultra Broadband Amplifier
Chart: 
120 nm
135 nm
Mazzler Trigger
The MAZZLER trigger has to be optimized carefully to center the optical pulse into the acousto-optic crystal

## Slide 12: Ultra Broadband Amplifier

## Slide 13: Ultra Broadband Amplifier
14.5 fs
Wizzler Feedback Loop is more efficient
than spider Loop
Measured Pulse Duration 14 fs

## Slide 14: CONCLUSION AND PERSPECTIVES
Chart: 
Pulses as short as 14 fs has been demonstrated directly at the output of
A Ti:Sa CPA laser system
Regenerative pulse with Mazzler has been extended to ultra broad spectra
Current limitation is due to the stretcher spectral transmission
A 180 nm Spectral transmission Stretcher has been developed
=> pulses has short has 10 fs could be obtained